Magnetizer.doc
                        9/29/2021 14:57:00 PM                                pg  4

Magnetizer Study

Bill Hart

802 Barkwood Dr NE

Cedar Rapids, IA 52402

21
General Information


21.1
Summary


21.2
References


21.3
Magnetic Units of Measure


21.3.1
H Field


21.3.2
B Field Flux Density


31.3.3
Field Total Flux


31.3.4
Field Energy


31.4
Properties of Air and Earth Field


31.5
Properties of Iron and Steel


31.5.1
Time to Magnetize Iron and Steel


41.6
Erasure of Permanent Field in Iron


41.7
Wire Resistance


41.8
LC Circuit Formulas


52
Circuit Considerations


52.1
Magnetism at Center of a Air Core Coil


62.2
Field Pattern of Air Core Coil


82.3
Ringing and Damping


92.4
Switch Contacts


92.5
Charging


102.6
Safety Discharge Resistor


103
Hoop-Coil Design Theoretical Examples


113.1
Battery – Not practical


113.2
Capacitor at 100V


123.3
Capacitor and Rectified AC Line (173V)


123.4
Capacitor and #22 AWG


123.5
Capacitor at 1000V


123.6
Smaller Coil, #22 AWG


133.7
Smaller Coil, #18 or #20 AWG


134
Iron Core Design Ideas


145
Experiments


145.1
Preliminary Test Methods


145.2
Preliminary Test Results


155.3
Working Coil Results, Known Target


165.4
Working Coil Results, Unknown Target


175.5
Small Radius Coil Results, Unknown Target




1 General Information

1.1 Summary

This study of magnetism and magnetizers has the goal of understanding the best way to magnetize a rebar that is buried at some depth in the ground, in order to facilitate locating it.

A moderately high-energy capacitor pulse circuit is needed (tens to hundreds of joules) unless a huge amount of copper is used in the coil.  Direct use of a battery does not seem practical, but charging capacitors needs only moderate battery capacity.  

Note that a magnetizer differs in principle from high energy can and quarter crushers in that magnetization depends on the strength of the field whereas the crushers depend on the rate of change of the field to induce currents in the target object. The magnetizer will generally have many more turns of wire in a large coil diameter.

The design process typically assumes a desired field strength, coil diameter, and voltage.  These dictate the size of wire needed. Wire size and coil diameter set a minimum capacitor size for a damped pulse, but a freewheeling diode would allow use of an underdamped pulse.  Often a larger capacitor will be used.  Usually many turns will be used in the coil to reduce the peak current and extend the pulse length.  Although counterintuitive, if source resistance is negligible and the capacitor large, the peak field strength is independent of the number of turns.

Tests, with a 17-inch diameter coil and pulse circuit that is expected to generate several times the earth’s magnetic field at a depth of up to two feet, demonstrated a significant improvement in magnetization of irons.

1.2 References

A handy calculation for magnetic field of a coil provided some of the results: https://tiggerntatie.github.io/emagnet/offaxis/iloopcalculator.htm
The FEMM finite-element modeling program is easy to use, and provides some guidance.  It is limited to a choice of planar or “axisymmetric” configuration, so interesting setups like an off-center rebar cannot be simulated; an off-center bar becomes a large-diameter pipe.

https://www.femm.info/wiki/HomePage
Magnetic Units of Measure

1.2.1 H Field

Amp-turns/meter is the SI unit for coercive force, i.e., magnetic potential gradient.

Oersted =1000/12.54 = 79.745 amp-turns/meter is an older unit.

1.2.2 B Field Flux Density

B = μ H        (Teslas, amp-turns/meter)

1 Tesla = 1 Weber /meter2 = 10,000 maxwells/cm2
Saturation flux for forms of iron is around 0.6 to 1.6 Tesla.

1 gauss = 100 μTesla   or 1 Tesla = 10,000 gauss

1 gamma = 1 nanoTesla

1.2.3 Field Total Flux

1 Weber = 1 Tesla-meter2 = 1 volt-second = 108 lines = 10 maxwells

1.2.4 Field Energy

The energy in the static magnetic field of a coil is E= ½ L I2    Joules. 

1 Joule/m3 = 0.126 kilo-gauss-oersted

1.3 Properties of Air and Earth Field

Air has a permeability close to that of vacuum, μ ≈ μ0 = 4π × 10−7 Henry/m.

Earth’s H field varies somewhat with location but is about 0.6 Oersted or less, 40-50 amp-turns/meter. In air, this produces a flux density B of between 40 and 60 μTesla (0.4 to 0.6 gauss).  

A magnetizer design should set a goal at least 1 to 2 orders of magnitude stronger H field to a buried rebar, thus inducing a flux density B in iron many times the earth’s field.

1.4 Properties of Iron and Steel

Most iron and steel have absolute permeability of μ ≥ 1.26×10−4 Henry/m, i.e., μr ≥100. Carbon steel may have μr  from 200 to 800 and annealed very pure iron and some alloys (including transformer silicon steel) may have μr as large as 5000.

Carbon steel with μr= 200 and aligned with the slanted earth’s field would have a flux density of 120 gauss, and if aligned vertically perhaps 85 gauss.

Carbon steel saturates at a flux density near 1.6 Tesla (16,000 gauss). Other forms of iron may saturate around 1.2 T.  The effective permeability falls dramatically as saturation is approached.

Most iron or steel materials need H = 2000 Amp-turns/meter (25 Oe) to develop the majority of possible permanent magnetization, and 3000  (37.5 Oe) to get near saturation. 

After the external field is removed, typically the remanent magnetization is half that achieved by the field.  Thus after saturation, carbon steel might retain up to 8000 gauss. (0.8 T).

On axis but somewhat away from the coil we may get a quarter to half of the center value. Thus after a pulse we should get significant remanent magnetization for a buried iron, perhaps several times that induced by the earth.

1.4.1 Time to Magnetize Iron and Steel

A posting on the internet said:

… the magnetic field takes time to penetrate the bulk iron structure. The rough estimate of the time to get the entire iron structure magnetized can be estimated from the skin depth formula. The frequency at which the skin depth equals the radius of the bar is the reciprocal of the time to penetrate the bulk. Because of the high permeability of the iron it can take milliseconds for the fields to reach the inside unless one uses intentionally excessive fields (e.g. ten times the needed H) to saturate the bulk even before full penetration.
By that rule a 5/8” diameter bar with skin depth= radius=8 mm at 15 Hz would take on the order of 60 msec to fully magnetize if below saturation. Saturated iron would have permeability near 1 and no longer seriously affect the field propagation into the center, speeding the process.

Experiments with tapping a permanent magnet against a rebar that was inside a 50-turn coil of wire found the induced coil voltage took 1 to 3 msec to peak and about 1 msec to decay. The voltage is proportional to the rate of change of flux inside the coil.  As the magnet gets closer, the flux increases faster. After contact, the flux is still increasing (voltage positive), but at a lower and lower rate. These times do not match the theory discussed above, but at least indicate that no longer pulse is needed.  

Industrial magnetizers often use a half-cycle of AC, thus a pulse width less than 8 msec near peak. Do they leave the material in the magnetizer for multiple half cycles? Do they use H high enough for saturation to reach the center before a weaker wave would propagate in?

1.5  Erasure of Permanent Field in Iron

An alternating magnetic field will cause the B-H curve to traverse back and forth and tend to erase any magnetization that had been induced in the iron, much like an eraser for tape recordings.  A rebar that is located under a large power line for many years may thus have any original magnetization removed, leaving only the earth field component and the AC ripple.

1.6 Wire Resistance

	AWG
	milliOhms per ft
	Ft per pound
	
	AWG
	milliOhms per ft
	Ft per pound

	30
	103
	3287
	
	16
	4.0
	128

	26
	40.8
	1300
	
	14
	2.52
	80.4

	22
	16.1
	514
	
	12
	1.59
	50.6

	20
	10.2
	323
	
	8
	0.63
	24.2

	18
	6.4
	203
	
	6
	0.40
	12.6


Table 1
1.7 LC Circuit Formulas

A solenoid coil of radius rcoil, length l, and radial winding thickness b has an inductance of approximately


[image: image1.wmf]b

l

r

N

r

L

in

coi

in

coil

10

9

6

8

.

0

,

2

2

,

+

+

»

 inches, L in microhenries

For a hoop coil with other dimensions negligible compared to the radius, a decent approximation is


[image: image2.wmf]8

2

,

N

r

L

in

coil

»

   radius in inches, L in microhenries or 
[image: image3.wmf]2

,

5

N

r

L

m

coil

»

 in meters

Thus for a 3-foot diameter hoop coil 
[image: image4.wmf]2

25

.

2

N

L

»

 μH.

The circuit’s resonant 
[image: image5.wmf]C

L

R

q

r

1

=

 with the critical damping value being qr=1/2.

The charge on the capacitor is 
[image: image6.wmf]t

I

V

C

Q

c

=

=

 coulombs = amp-seconds

Energy = 
[image: image7.wmf]2

2

1

CV

E

=

 joules.

For example at 1000 μF and 100 volts the capacitor holds 5 joules = 5 watt-seconds, which is a dangerous shock hazard but not a lot of energy from a heating standpoint.

2 Circuit Considerations

2.1 Magnetism at Center of a Air Core Coil
A hula-hoop-size air core coil laid on the ground would cover lots of area and the field fall-off is gradual enough to allow useful penetration depth (see graph in section 2.2.  A smaller coil (section 5.3) may be useful. Generating a strong enough field requires a moderately high-energy discharge into the coil.

R0  is the resistance of the source battery or capacitor ESR, connecting wire, and switch

Rt = ohms per turn      and R = Rt N is the coil resistance

rcoil,m = radius in meters


[image: image8.wmf]m

coil

r

I

N

Bcenter

,

2

m

=

 Teslas flux at center of coil, or 
[image: image9.wmf]m

coil

r

I

N

Hcenter

,

2

=

 amp-turns /meter


[image: image10.wmf]L   N turns

R (wire)

R

0

C

Charge to

V volts

I

free-

wheeling

diode

-Charge

-Fire

-Safe

Rsafe


With a steady state voltage, or early part of a capacitor discharge (neglecting inductance),


[image: image11.wmf](

)

÷

ø

ö

ç

è

æ

+

=

+

=

N

R

R

r

V

R

R

N

r

V

N

H

t

m

coil

t

m

coil

center

0

,

0

,

2

2

    


[image: image12.wmf]H field versus N turns

0

0.1

0.2

0.3

0.4

0.5

0.6

0.7

0.8

0.9

1

0

5

10

15

20

25

30

35

N turns

Relative H value

R0 = Rt

R0 = 10 Rt


We usually use enough turns 
[image: image13.wmf]t

R

R

N

0

>>

 of a given size wire to swamp out the source resistance.  More turns give diminishing improvement in H but reduces the current.

If we neglect R0, we can find the minimum size of wire from 
[image: image14.wmf]center

m

coil

t

H

r

V

R

,

2

=

 ohms per turn REGARDLESS OF N TURNS.  This usually comes out to be a larger size wire than we would like.

The current is likely to be larger than we want with a small number of turns. 
[image: image15.wmf]0

R

R

N

V

I

t

+

=

  

We can reduce the current and extend the pulse time without much change in H by using more turns of the chosen wire size, if the new bulk and cost are acceptable, because the additional turns multiply the field proportionally to the multiplied resistance, thus nearly constant amp-turns. 


[image: image16.wmf]Decrease in current with more turns (R

0

 = 10 R

t

)

0

0.25

0.5

0.75

1

0

5

10

15

20

25

30

35

40

45

50

N turns

Relative current


More turns will make the pulse last longer due to draining the capacitor more slowly, and also the increased inductance L~N2 will slow the rise and fall times (see also the section on ringing).

2.2 Field Pattern of Air Core Coil


[image: image17.wmf]Fall-off of field along coil axis

0

0.2

0.4

0.6

0.8

1

1.2

0

0.5

1

1.5

2

2.5

Distance Z from coil center / radius

Flux/center flux  


At the center of the air-core coil the flux density would be


[image: image18.wmf]m

coil

r

I

N

Hcenter

Bcenter

,

2

m

m

=

=

 Teslas flux at center of coil

At a distance Z along the axis of the loop (into the ground) the field falls off as 
[image: image19.wmf]2

/

3

2

,

1

1

÷

÷

ø

ö

ç

ç

è

æ

+

÷

÷

ø

ö

ç

ç

è

æ

=

m

coil

center

Z

r

Z

B

B

 

This shows that a coil laid on the ground should get moderate penetration into the ground for a distance on the order of the radius.  If a rebar is located in the vicinity it will pull in much more flux and distort the field so this equation is pessimistic.

Radially, the vertical component of the field in the absence of iron is different at different depths according to the following figure.


[image: image20.wmf]Vertical component of field (no iron) of 18" = 0.457 m radius loop 

-10

0

10

20

30

40

50

0

0.2

0.4

0.6

0.8

1

Radial distance from center, meters

Flux, Gauss

In plane of coil

0.5 radius below coil

1 radius below coil


If we assume some fixed V and wire size, there is an optimum radius of at least 0.7 times the depth we are interested in, but it is non-critical for a range of radii.  A larger coil gives better penetration and coverage area at depth, but the increased wire resistance per turn reduces the current and thus less field nearer the surface. For this project we want rcoil > 0.2 m or a diameter of at least 16”, and 24” would be good for coverage at depth.

For example, the following chart shows 200 volts, and #22 wire. For other electrical parameters only the amp-turns/meter scaling changes and the size relationship holds.


[image: image21.wmf]Field along coil axis versus coil radius, #22 AWG, 200V

0

200

400

600

800

1000

1200

1400

1600

1800

2000

0

0.2

0.4

0.6

0.8

1

Coil Radius, m

Amp-turns/meter

Earth field

Depth, m

0

0.25m=10"

0.30m=12"

0.40m=16"

0.50m=20"

0.75m=30"


When an iron is placed in the field, it increases the flux density. The simulation shows lines of constant density in a half-plane slice through a bar with a coil above it.


[image: image22.wmf] 


2.3 Ringing and Damping

If the circuit rings, so the current momentarily reverses, we risk losing some magnetization that has been induced in the iron and possibly damaging the capacitor.  Thus we need to either be damped at or beyond critical damping factor, or else provide a free-wheeling diode across the coil.  If we are using high voltage, it may not be practical to find a diode with adequate voltage and current capability.

More turns do not change the damping so long as stray effects and R0 can be ignored.  The increased R=N Rt  and L = N2 Lt will extend the pulse.

 
[image: image23.wmf]C

L

R

C

L

N

NR

C

L

R

q

t

t

t

t

r

1

1

1

2

=

=

=

              
[image: image24.wmf]LC

f

p

2

1

0

=

 

Using the time constants 
[image: image25.wmf]RC

RC

=

t

and 
[image: image26.wmf]R

L

RL

=

t

 we find 
[image: image27.wmf]RC

RL

r

q

t

t

=


If we want critical damping, qr = 0.5 or overdamping

Set 
[image: image28.wmf]2

min

min

2

1

2

1

÷

ø

ö

ç

è

æ

=

=

=

t

t

t

t

r

R

C

L

C

L

R

q

   
[image: image29.wmf]2

min

4

t

t

R

L

C

=

 μF, μH, ohms         
[image: image30.wmf]RL

RC

t

t

4

³


Using the inductance approximation for a hoop coil, 
[image: image31.wmf]2

,

2

,

.

2

min

20

2

8

4

t

m

coil

t

in

coil

in

coil

t

R

r

R

r

r

R

C

=

=

»

 uF

Since resistance per turn is proportional to the coil radius, a larger coil can use a smaller capacitor and the same wire size while remaining critically damped.

If we use a larger capacitor than this, as would be likely for moderate voltage, the pulse will be longer and overdamped as L becomes unimportant.

In terms of our principal specifications V and Hcenter, and solving out Rt, critical damping requires 
[image: image32.wmf]2

,

,

min

2

20

÷

÷

ø

ö

ç

ç

è

æ

»

V

H

r

r

C

center

m

coil

m

coil

     
[image: image33.wmf]2

2

3

,

min

80

V

H

r

C

center

m

coil

»

uF (meters, A-t/m, volts)

Iron in the coil field will increase the inductance and make it less damped.

2.4 Switch Contacts

Most of the designs considered here have initial currents in the tens to a hundred amps, quickly reducing toward zero. If the contacts bounce, the inductance will tend to keep the current flowing across the momentary open to create excessive voltage and arc. Both the high current and possible arcing will be hard on switch contacts.  Using a freewheeling diode across the coil would tend to alleviate the arcing problem, as the switch would never see more than the capacitor voltage.

2.5 Charging

Calculations in section 3.1 below indicate that a 12-volt battery cannot drive a practical coil to sufficient field strength.  Many on-line sources offer a “DC to DC Step up Boost Converter” for $10 to $15 that will take a battery input and make higher voltage.

Some experiments were done with a stack of used 9V batteries that were on hand.

If AC power is available at the location of interest (near buildings or from a small inverter from a vehicle battery) a rectifier circuit can be used.

The charging circuit could be a simple resistor and diode with an AC plug, assuming everything was isolated from ground and not touched while plugged in for charging.  For better safety, two small transformers could be used to step down and back up to isolated line voltage. A full wave bridge would cut the charge time to about half.


[image: image34.wmf]L   N turns

R (wire)

R

0

Charge to

173 volts

I

-Charge

-Operate

-Safe

Rsafe

24 V

100 ohms

Fire


2.6 Safety Discharge Resistor

Designs using a high voltage capacitor should incorporate a safety discharge resistor to prevent the capacitor from building a dangerous voltage as stored charge resurfaces, and also as a means to discharge the capacitor if the coil becomes disconnected.

The most robust resistors would be wirewound, but may not be available with high enough resistance.  Bulk carbon resistors would be next best, and film resistors should be avoided because of the concentration of power in a thin layer, which requires time to dissipate heat.

Although the energy to be dissipated is moderate, a carbon resistor should not be stressed with excessive instantaneous power.  Perhaps a short pulse could be 10 times the steady-state rating but not 100 times? 

The chosen resistance should form an RC time constant on the order of seconds. For example, to discharge a 100 uf capacitor charged to 1000 volts with a time constant of 10 seconds needs 100 k ohms; the initial current would be 10 ma and the initial power would be 10 watts.  Section 3.6 gives another Rsafe example.

Also, at high voltages it is possible for arcing to occur between grains of the resistor rather than conduction being entirely through particle contact surfaces so a series string of resistors could be advantageous.

The switch contacts used for the safety resistor will not see large currents nor an inductive load.

3 Hoop-Coil Design Theoretical Examples

Some examples will show the range of parameters to consider.  Unless otherwise indicated, all hoop coil examples use a goal of 2000 amp-turns and a 36-inch diameter coil (18” radius, 0.457 meter), 9.4 ft circumference, L=2.25 N2 μH.  Thus the initial current will be 2000/N amps. 

At the center of the air-core coil Hcenter = 2188 A-t/m and the flux density would be 
[image: image35.wmf]0027

.

0

457

.

0

2

2000

0

=

=

x

Bcenter

m

 Teslas = 27.5 gauss. This is on the order of 50 times the flux from the earth’s magnetic field (typically 0.5 gauss). It is approximately the field over much of the plane inside the coil except close to the wire (see section 2.2 above).  

Along the axis of the loop at a distance (into the ground) the field drops according to the formula and graph given in section 2.2.  At distance equal to the radius it is 9.7 gauss and corresponds to 770 amp-turns/meter in air, or more near any iron.

A simulation of a pipe at depth slightly more than the coil radius shows the flux pattern. This view is like a lemon slice that reveals the pattern in the whole lemon. The additional tall boxes in the figure were air for this run, but could be selected as steel to see the effect of additional “helper” irons as mentioned in section 4.

[image: image36.jpg]


[image: image37.jpg]



3.1 Battery – Not practical

For 12-volt battery we need 
[image: image38.wmf]H

V

R

t

=

< 6 milliohms per turn or 0.64 milliohms per foot, which is about #8 AWG, and we are not going to use a huge number of turns at that size. The current drain for a fat coil of N=10 turns (94 ft, 3.9 pounds of wire) would be 200 amps if the battery could supply that (low R0).

A higher voltage battery would likely have a seriously larger source resistance (lower short circuit current).  Such a battery should be used to charge a capacitor at a higher voltage.

3.2 Capacitor at 100V

If we use a 100-volt charge on a capacitor (a common component rating) we get 0.05 ohm per turn and 5.3 milliohms per foot, which is about #16 AWG. The minimum C for damping is 3050 μF. Such a capacitor may have that much ESR itself (aluminum electrolytic 50 to 100 milliohm), so we would need several turns to make R0 negligible. It would discharge any practical size of capacitor much too quickly with small N

If, for example, we have 5000 μF, the RC time constant is 0.25 N milliseconds.  N=20 may be practical for 900 μH (190 ft, 1.5 pounds of wire) which would reduce the effect of ESR and give maybe 90% of target H. The resonant frequency is 75 Hz and the half-cycle 6.7 msec may be long enough for the iron domains to align.  Damping is q=0.42 (neglecting capacitor ESR), just about right.  Initial current is 100 amps, which may exceed simple switch ratings and pit or weld contacts, even though brief.

With 5000 μF and 100 V we have 25 joules.  The charge is 0.5 Coulomb = 0.5 amp sec so a constant 100A would drain it in 5 msec (an order of magnitude check on frequency and damping values). Charging might take 20 seconds at initial current 50 mA (5 watts).

Capacitor and Rectified AC Line (173V)

Consider 3000 μF at 173 volts (peak of household AC). We need 88 milliohms per turn and 9.4 milliohms per foot; 18 AWG is a little lower R at 6.4 milliohms/ft or 60 milliohms per turn.  

N=20 may be practical but marginal, for 900 μH (190 ft, almost 1 lb of wire) and 1.2 ohms total. If this is 3x 1000 μF the parallel combination ESR should be less than 30 milliohms, R0 ~ 0.5 Rt and gives an initial current of 143 amps, or 2860 amp-turns.  The RC time constant is 3.6 msec. More turns might be desirable to more fully overcome Rt, reduce the current, and extend the pulse time. Damping is q=0.46, acceptable, but more C is desirable for pulse length.

3.3 Capacitor and #22 AWG

This wire has 16.1 milliohms per foot, or 0.15 ohms per turn.  To get 2000 A-t we need 300 volts.  The ESR of suitable capacitors needs to be investigated.

An alternative would be to wind parallel turns of #22, to get 0.075 ohm/turn.  Then 150 volts minimum would get our goal for amp-turns and 173 volts would be better.  This would take a lot of turns to slow down the capacitor discharge. N=40 (wire 80 times circumference = 754 ft, 1.5 pounds) would give a time constant of a few msec.  Is there a “shorted-turn” problem if the placement of parallel turns is not symmetric?

3.4 Capacitor at 1000V

At 1000 V we could stand 0.5 ohm per turn or 0.053 ohms per foot, so 26 AWG wire could be used, the size making it easier to use more turns.  At this initial voltage, there is risk of arcing if the start and finish winding are close together. Critical damping would occur at C=36 μF.  A 100 μF capacitor would give a time constant of about 50N microseconds. N=100 then would give an initial current of 20A and a 5 msec pulse, overdamped so the (expensive?) diode would not be needed unless for switch bounce.  More C is desirable for a longer pulse.

With 100 μF and 1000 V we have 50 joules, so heating should be considered.

3.5 Smaller Coil, #22 AWG

This example does not follow the parameters of the others. Readily at hand are three 1000-μF 200-volt capacitors and a spool of #22 wire (16.1 milliohms/ft).  If the charging circuit used rectified household AC with 173 volt peak the energy is 45 joules. The goal of 2000 a-t would require Rt = 86.5 milliohms per turn, so we could have a circumference of 5.37 ft or a diameter of 20 inches. R0=ESR would be expected to be somewhat less than Rt.

This coil would be large enough to conduct practical experiments, but would require 4 times as many attempts as the other example coils for searching a larger area and would only project about half as far into the ground as the other examples.

An RC discharge time constant of 10 msec would require a total resistance of 3.3 ohms, which would be 205 feet of wire or 38 turns minimum. L= 1805 μH and resonance 68 Hz. Damping qr=0.23, overdamped so no freewheeling diode is needed unless for switch bounce.  Initial current would be 53 amps. More turns, say 75 (334 ft, 0.65 pound), would be better.

The charge would be 0.52 coulombs = amp-seconds. To charge from 120V rms through 2700 ohms gives an initial current 45 ma that would initially dissipate 5.5 watts and fall to zero, so a 1-watt wirewound resistor might serve. Alternatively a 100-ohm resistor in a 24-volt portion of the isolation circuit or 68 ohms at 20V would give similar results.  The time constant is 8 sec but initially half duty cycle and reducing to a very small duty cycle as the capacitor voltage approaches the AC peak, so we might need most of a minute to approach full charge. A full wave bridge would cut the time to about half.

Rsafe should be a few K ohms and perhaps a 5-watt resistor.  If we use 2 K to dump a full charge (for example, if the coil became disconnected), the time constant is 6 seconds, the initial current is 87 ma, and the initial power is 15 watts.  With 6.8 K it is 20 seconds, 25 ma, and 4.4 watts.

See sections 5.3 and 5.4 for results with a similar coil.

3.6 Smaller Coil, #18 or #20 AWG

A 17-inch diameter (similar to the experimental coil below) (radius 0.216 meter) with #18 wire would have 4.45 ft per turn and 28.5 milliohms per turn.  At 200 volts, we would have 7021 amp-turns and 16,250 A-t/m in the plane of the coil. This would extend a large field to greater depth. The initial current would be 7021/N amps and we might consider 200 turns to get 35 amps. That would take 890 ft of wire, 4.4 pounds, which would cost in the range of $50.

Going to #20 wire would give results intermediate between 18 and 22, and would be more affordable than #18. Rt=45.4 milliohms/turn, 4400 A-t and 10,200 At/m. Using 112 turns (500 ft, 1.55 lb) gets 5.1 ohms and 39 amps. A slightly larger diameter could also be considered.

4 Iron Core Design Ideas

If we add an iron core to a small diameter coil, it is easier to develop high field strength in the vicinity of the core, but the field will not extend far radially.  If we saturate the iron, which would be easy to do, any additional field would be particularly limited in area by the small coil diameter.

Finite element simulations indicate that adding massive iron above the ground inside a large coil provides minimal improvement at depth.  A single added rod in the center of the coil, with the rod extending somewhat above the coil and as far as practical downward, is quite effective if it is radially close to a buried rebar, even if it is still somewhat above it. 

Driving iron rods into the ground all around the inside of a large coil (where field is strongest) will extend the field further into the ground.  Removing them before searching with the locator could find enhanced magnetism on a deep rebar or pipe.  As mentioned with the reference link, the FEMM simulation program is limited in the configurations that can be simulated, so it cannot study the improvement with a small number of additional rods.

Using a small diameter coil with a helper rod in its center and driven into the ground can extend the field downward in a small region.  If the expected location of a buried iron is known, driving the helper rod close by could help.

Simulation with an electrician’s spool of #12 wire as in section 5.1, 142 volts, 200 amps, 100,000 A-t are more than enough to saturate an iron rod in the center of the spool. If extending 0.2 meter (8”) into the ground, it could induce perhaps 400 gauss into a buried rod whose top was 0.4 meter (16”) down, or 200 gauss if it were 0.5 meter (20”) down. This is still more than double the flux induced by the earth field, so would produce a marginal improvement.  A thicker helper iron does somewhat increase the field at depth, but principally the depth is what is important.  An iron plate laid over the coil produces a small improvement.

5 Experiments

5.1 Preliminary Test Methods

Before winding a coil, preliminary experiments were done with a spool of electrician’s #12 wire and a 14 inch, #4 rebar (nominal ½” before serious rusting).   A capacitor bank of 12 x 820 = 9840 μF charged from a stack of used 9V batteries achieved 142 V.  This is 1.4 amp-seconds and 99 joules. It was discharged into the coil by touching wires together, which caused the wire to jump and sometimes produced a spark. A better switch should be used but the current may be excessive.

The rebar was demagnetized with a tape recorder eraser and the unmarked end was placed in the spool lying on a table with the marked end sticking up.  Thus the entire rebar may not be affected to the same degree.

Magnetic readings used a Samsung cell phone with a “Metal Detector” app that reads out the field in arbitrary units on a scale that goes at least to 3000. It may be grossly 2000 units per tesla. It does not appear to read out polarity, so a compass was used for that.  Readings vary somewhat with exact placement of the phone on edge at the end of the rebar. Readings were taken at each end of the rebar, with the measured end up, after each of multiple pulses without erasing. It was later learned that holding the phone flat gets the rod closer to the sensor and reads higher, so the values had been taken at some small additional fixed distance.

Very approximate values were 0.6 ohm of #12 wire plus 0.1 ohm of clip lead connecting things. This calculates to 377 ft of wire.  

The spool has 1” inner radius, 1.65” outer radius, and 4.6” long, for an average radius of 1.32”.  The average turn length is then 0.69 ft, indicating 546 turns and 1.1 milliohm per turn average.

The initial current ignoring inductance and R0 would be 202 amps and produces 110,000 amp-turns, which are spread over the 4.6 inch = 0.117 m length of the coil (nearly twice the mean diameter), with each turn adding in accordance with the above figure shifted according to its position.  This will probably result in less than ¼ of the H field at any point compared to a compact coil having the same amp-turns.

The RC time constant is 6.9 msec, but the inductance would be on the order of 7500 μH and makes it underdamped q=1.2, with a resonance of 18.5 Hz or half cycle of 27 msec. The peak current will be reduced because the capacitor is partly discharged before the inductor lets the current peak. 

Preliminary Test Results

Initial attempts gave varying results, so a freewheeling diode was added to deal with ringing and the results became consistent. Alternatively, a 1-ohm additional R0 might be tolerable to provide that damping with a loss in peak current.

	Pulse Cycle

142 V
	Marked end

out of coil
	Unmarked end

in coil

	Air no rebar
	76
	

	Erased rebar
	N 167
	N 150

	1 pulse
	S 1020
	N 1310

	2
	S 1010
	N 1290

	3
	S 1020
	N 1325


Table 2  Experimental Magnetic readings (arbitrary units)

The setup should produce a peak H field far over that needed in steady state to saturate the iron. Multiple pulses did not change significantly the strength, showing the pulse was long enough.

Further experiments at lower voltage showed that nearly the same values could be reached.  With only 7.6 V repeated a few times, readings of 567 x 1183 were reached. This shows that one end reached near saturation, but with the lower voltage (5920 amp-turns spread over 4.6 inches would give 1000 to 2000 amp-turns/meter) saturation had not propagated to the end of the rebar outside the coil.

From this we can conclude that 1175 of these units is the remanent magnetization after saturation, aided or bucked by the earth field.  This is 7.5 times the flux induced by the earth, ± the earth field. This is a disappointment, as estimates in section 1.5 suggested 20x.

5.2 Working Coil Results, Known Target

Using parts on hand, a 17” (0.432 meter) diameter coil of #22 AWG wire with 75 turns (334 ft of wire) was tested.  A bank of 12 x 820 = 9840 μF charged from a stack of used 9V batteries achieved 142 V. Charge is 1.4 coulombs = amp-seconds, and energy 99 joules = watt-seconds. 

The circumference is 4.45 ft, which at 16.1 milliohms/ft makes Rt = 72 milliohms/turn and the total R=5.37 ohms.  RC = 53 msec.  Inductance is about 5976 μH, L/R = 1.1 msec, and resonant frequency 20.7 Hz, half cycle 24 msec, and q = 0.14 overdamped. Inductance would increase with iron close to coil.

At 142 volts the initial current is 26 amps (slightly less with inductive rise), readily handled by an ordinary switch.  This would produce almost 1983 amp-turns, and H= 4600 amp-turns/meter at the center of the coil.  This is 59 gauss in air or over 100 times the earth field, and should saturate iron near the coil. 

At a depth of 1 foot (0.3048 meter) this should produce over 10 gauss (20x earth field). At a half-meter (20 inches) we calculate 270 a-t/m or 3.5 gauss (7x earth field). At two feet (0.61 m) we expect 2.1 gauss (4x earth field).  An iron bar should pull in more of the field than that and retain perhaps half of what it experiences.

An initial trial with one end of the 14” rebar (#4 size) at the center of the coil gave a scale reading of 930 arbitrary units, and after four pulses 968.  This is about 73% of the remanent magnetization achieved by saturation as measured in section 5.2.  This is not quite consistent with the preliminary test, but in the ballpark.

 The other end of the rebar (1.65 coil radii away) measured 531 units or 40% of maximum. This is more than predicted by the curve in section 2.1 because the iron pulls in more of the flux than would be in that position in air.

Experiments on a real lot corner that has a #5 rebar flush with the ground, coil on ground centered on rebar, at 167 volts, got (edge of phone) readings of 1982 units North. Some of the older batteries were getting tired after several attempts to reverse it, and with the coil 6 inches above ground it would mostly erase but not fully magnetize in the opposite direction.  At 3 inches and 145 volts it got 520 units S. This is mildly disappointing.

For comparison, after a speaker magnet touch the rebar read 931 units. 

5.3 Working Coil Results, Unknown Target

[image: image39.jpg]



The 17” diameter coil was tried at a location that was hoped to have a rebar, somewhat deeper than usual due to possible fill, and under a power line that makes enough hum in the magnetic locator to obscure small signals.  Using enough batteries to get 190-200V produces 35-40% more amp-turns than the prior experiments, 2790 A-t, 6430 A-t/m (see figure in section 2.2 at depths).

With 190 volts, a previously unfound vertical 10d nail was found at 6-inch depth.  After replacing the nail with a non-metallic rod no rebar was sensed below it, so the nail was put back.

[image: image40.jpg]



5.4 Small Radius Coil Results, Unknown Target

A brief experiment was done with the spool of electrician’s wire discussed in section 5.2 and the pulse circuit of the previous section.  Small iron rods were inserted through its center and pushed to a depth of over a foot.  No additional iron was detected after several pulses.

_1691922234.unknown

_1691922325.unknown

_1692464293.xls
Chart1

		1		1

		2		2

		3		3

		4		4

		5		5

		6		6

		7		7

		8		8

		9		9

		10		10

		11		11

		12		12

		13		13

		14		14

		15		15

		16		16

		17		17

		18		18

		19		19

		20		20

		21		21

		22		22

		23		23

		24		24

		25		25

		26		26

		27		27

		28		28

		29		29

		30		30

		31		31

		32		32

		33		33

		34		34

		35		35

		36		36

		37		37

		38		38

		39		39

		40		40

		41		41

		42		42

		43		43

		44		44

		45		45

		46		46

		47		47

		48		48

		49		49

		50		50

		51		51

		52		52

		53		53

		54		54

		55		55

		56		56

		57		57

		58		58

		59		59

		60		60

		61		61

		62		62

		63		63

		64		64

		65		65

		66		66



R0 = Rt

R0 = 10 Rt

N turns

Relative H value

H field versus N turns

0.5

0.0909090909

0.6666666667

0.1666666667

0.75

0.2307692308

0.8

0.2857142857

0.8333333333

0.3333333333

0.8571428571

0.375

0.875

0.4117647059

0.8888888889

0.4444444444

0.9

0.4736842105

0.9090909091

0.5

0.9166666667

0.5238095238

0.9230769231

0.5454545455

0.9285714286

0.5652173913

0.9333333333

0.5833333333

0.9375

0.6

0.9411764706

0.6153846154

0.9444444444

0.6296296296

0.9473684211

0.6428571429

0.95

0.6551724138

0.9523809524

0.6666666667

0.9545454545

0.6774193548

0.9565217391

0.6875

0.9583333333

0.696969697

0.96

0.7058823529

0.9615384615

0.7142857143

0.962962963

0.7222222222

0.9642857143

0.7297297297

0.9655172414

0.7368421053

0.9666666667

0.7435897436

0.9677419355

0.75

0.96875

0.756097561

0.9696969697

0.7619047619

0.9705882353

0.7674418605

0.9714285714

0.7727272727

0.9722222222

0.7777777778

0.972972973

0.7826086957

0.9736842105

0.7872340426

0.9743589744

0.7916666667

0.975

0.7959183673

0.9756097561

0.8

0.9761904762

0.8039215686

0.976744186

0.8076923077

0.9772727273

0.8113207547

0.9777777778

0.8148148148

0.9782608696

0.8181818182

0.9787234043

0.8214285714

0.9791666667

0.8245614035

0.9795918367

0.8275862069

0.98

0.8305084746

0.9803921569

0.8333333333

0.9807692308

0.8360655738

0.9811320755

0.8387096774

0.9814814815

0.8412698413

0.9818181818

0.84375

0.9821428571

0.8461538462

0.9824561404

0.8484848485

0.9827586207

0.8507462687

0.9830508475

0.8529411765

0.9833333333

0.8550724638

0.9836065574

0.8571428571

0.9838709677

0.8591549296

0.9841269841

0.8611111111

0.984375

0.8630136986

0.9846153846

0.8648648649

0.9848484848

0.8666666667

0.9850746269

0.8684210526



Sheet1

		N		R0 = 10 Rt				R0 = Rt

		1		0.0909090909				0.5		10		0

		2		0.1666666667				0.6666666667		10		1

		3		0.2307692308				0.75

		4		0.2857142857				0.8

		5		0.3333333333				0.8333333333

		6		0.375				0.8571428571

		7		0.4117647059				0.875

		8		0.4444444444				0.8888888889

		9		0.4736842105				0.9

		10		0.5				0.9090909091

		11		0.5238095238				0.9166666667

		12		0.5454545455				0.9230769231

		13		0.5652173913				0.9285714286

		14		0.5833333333				0.9333333333

		15		0.6				0.9375

		16		0.6153846154				0.9411764706

		17		0.6296296296				0.9444444444

		18		0.6428571429				0.9473684211

		19		0.6551724138				0.95

		20		0.6666666667				0.9523809524

		21		0.6774193548				0.9545454545

		22		0.6875				0.9565217391

		23		0.696969697				0.9583333333

		24		0.7058823529				0.96

		25		0.7142857143				0.9615384615

		26		0.7222222222				0.962962963

		27		0.7297297297				0.9642857143

		28		0.7368421053				0.9655172414

		29		0.7435897436				0.9666666667

		30		0.75				0.9677419355

		31		0.756097561				0.96875

		32		0.7619047619				0.9696969697

		33		0.7674418605				0.9705882353

		34		0.7727272727				0.9714285714

		35		0.7777777778				0.9722222222

		36		0.7826086957				0.972972973

		37		0.7872340426				0.9736842105

		38		0.7916666667				0.9743589744

		39		0.7959183673				0.975

		40		0.8				0.9756097561

		41		0.8039215686				0.9761904762

		42		0.8076923077				0.976744186

		43		0.8113207547				0.9772727273

		44		0.8148148148				0.9777777778

		45		0.8181818182				0.9782608696

		46		0.8214285714				0.9787234043

		47		0.8245614035				0.9791666667

		48		0.8275862069				0.9795918367

		49		0.8305084746				0.98

		50		0.8333333333				0.9803921569

		51		0.8360655738				0.9807692308

		52		0.8387096774				0.9811320755

		53		0.8412698413				0.9814814815

		54		0.84375				0.9818181818

		55		0.8461538462				0.9821428571

		56		0.8484848485				0.9824561404

		57		0.8507462687				0.9827586207

		58		0.8529411765				0.9830508475

		59		0.8550724638				0.9833333333

		60		0.8571428571				0.9836065574

		61		0.8591549296				0.9838709677

		62		0.8611111111				0.9841269841

		63		0.8630136986				0.984375

		64		0.8648648649				0.9846153846

		65		0.8666666667				0.9848484848

		66		0.8684210526				0.9850746269






_1692544676.xls
Chart1

		0		0		0		0		0		0		0		0

		0.05				0.05		0.05		0.05		0.05		0.05		0.05

		0.1				0.1		0.1		0.1		0.1		0.1		0.1

		0.15				0.15		0.15		0.15		0.15		0.15		0.15

		0.175				0.175		0.175		0.175		0.175		0.175		0.175

		0.2				0.2		0.2		0.2		0.2		0.2		0.2

		0.216				0.216		0.216		0.216		0.216		0.216		0.216

		0.25				0.25		0.25		0.25		0.25		0.25		0.25

		0.275				0.275		0.275		0.275		0.275		0.275		0.275

		0.3				0.3		0.3		0.3		0.3		0.3		0.3

		0.35				0.35		0.35		0.35		0.35		0.35		0.35

		0.4				0.4		0.4		0.4		0.4		0.4		0.4

		0.432				0.432		0.432		0.432		0.432		0.432		0.432

		0.5				0.5		0.5		0.5		0.5		0.5		0.5

		0.6				0.6		0.6		0.6		0.6		0.6		0.6

		0.7				0.7		0.7		0.7		0.7		0.7		0.7

		0.8				0.8		0.8		0.8		0.8		0.8		0.8

		0.9				0.9		0.9		0.9		0.9		0.9		0.9

		1				1		1		1		1		1		1

		0.216				0.216		0.216		0.216		0.216		0.216		0.216

		0.216				0.216		0.216		0.216		0.216		0.216		0.216

		0.457				0.457		0.457		0.457		0.457		0.457		0.457

		0.457				0.457		0.457		0.457		0.457		0.457		0.457



Earth field

Depth, m

0

0.25m=10"

0.30m=12"

0.40m=16"

0.50m=20"

0.75m=30"

Coil Radius, m

Amp-turns/meter

Field along coil axis versus coil radius, #22 AWG, 200V

45

0

45

120523.052432638

909.0967399287

535.5099396453

229.9853049287

118.737544008

35.4737796156

45

30130.7631081594

1543.4875158351

952.8183906076

429.8696154858

227.2741849822

69.5579692848

45

13391.4502702931

1823.7823208165

1197.7677248673

579.7050542587

317.7251768672

101.010748881

45

9838.6165251133

1855.4478442374

1258.6129332337

633.5463521121

354.6979203621

115.4326949462

45

7532.6907770399

1836.3452188003

1285.6569391163

673.7443452379

385.8718789588

128.8559715494

45

6458.0682244855

1804.647828044

1288.3113275243

692.7744363084

402.7950986791

136.8898012026

45

4820.9220973055

1704.4533532884

1264.8684912675

717.7201127556

431.1963809522

152.4509424972

45

3984.233138269

1614.1146834916

1229.2889786086

724.4539313042

445.9295105341

162.5489564376

45

3347.8625675733

1517.842189521

1183.6481620058

723.1383145958

455.9455802041

171.4986128706

45

2459.6541312783

1325.319484006

1076.5638034906

702.3450033741

463.8619610594

186.0125806975

45

1883.17269426

1148.3521804089

964.1844194611

665.8020911283

459.0863047001

196.2516628254

45

1614.5170561214

1046.816417479

894.6622079017

637.8314556097

451.161957011

200.7535858448

45

1205.2305243264

862.3927619045

759.9093003402

573.8578808751

426.1133383221

205.7051102586

45

836.9656418933

658.2961443749

598.8838624337

482.1213521686

379.4605473803

204.0383576445

45

614.9135328196

513.5819447473

477.4920889917

402.4742836252

331.3298710015

195.3327274677

45

470.793173565

409.3837738029

386.4700361725

336.8721726189

287.0880451022

182.7984422165

45

371.9847297304

332.7395975419

317.6061302025

283.8540133709

248.4813755292

168.649132169

45

301.3076310816

275.1165539109

264.7709807226

241.1699243492

215.5981904761

154.2695071138

0

5000

0

5000



Sheet1

		

		V		ohms/ft

		200		0.0161

		Depth, m		0.00		0.25		0.30		0.40		0.50		0.75

		Label		0		0.25m=10"		0.30m=12"		0.40m=16"		0.50m=20"		0.75m=30"		Earth field

		Radius, m		A-t/m		A-t/m		A-t/m		A-t/m		A-t/m		A-t/m		Earth

		0														45

		0.05		120523.1		909.1		535.5		230.0		118.7		35.5		45

		0.1		30130.8		1543.5		952.8		429.9		227.3		69.6		45

		0.15		13391.5		1823.8		1197.8		579.7		317.7		101.0		45

		0.175		9838.6		1855.4		1258.6		633.5		354.7		115.4		45

		0.2		7532.7		1836.3		1285.7		673.7		385.9		128.9		45

		0.216		6458.1		1804.6		1288.3		692.8		402.8		136.9		45

		0.25		4820.9		1704.5		1264.9		717.7		431.2		152.5		45

		0.275		3984.2		1614.1		1229.3		724.5		445.9		162.5		45

		0.3		3347.9		1517.8		1183.6		723.1		455.9		171.5		45

		0.35		2459.7		1325.3		1076.6		702.3		463.9		186.0		45

		0.4		1883.2		1148.4		964.2		665.8		459.1		196.3		45

		0.432		1614.5		1046.8		894.7		637.8		451.2		200.8		45

		0.5		1205.2		862.4		759.9		573.9		426.1		205.7		45

		0.6		837.0		658.3		598.9		482.1		379.5		204.0		45

		0.7		614.9		513.6		477.5		402.5		331.3		195.3		45

		0.8		470.8		409.4		386.5		336.9		287.1		182.8		45

		0.9		372.0		332.7		317.6		283.9		248.5		168.6		45

		1		301.3		275.1		264.8		241.2		215.6		154.3		45

		0.216				0

		0.216				5000

		0.457						0

		0.457						5000






_1694326440.unknown

_1692717452.doc
[image: image1.png]






_1692513551.xls
Chart1

		0		0		0

		0.1		0.1		0.1

		0.2		0.2		0.2

		0.25		0.25		0.25

		0.3		0.3		0.3

		0.35		0.35		0.35

		0.37		0.37		0.37

		0.4		0.4		0.4

		0.43		0.43		0.43

		0.45		0.45		0.45

		0.456		0.456		0.456

		0.46		0.46		0.46

		0.47		0.47		0.47

		0.48		0.48		0.48

		0.49		0.49		0.49

		0.5		0.5		0.5

		0.52		0.52		0.52

		0.55		0.55		0.55

		0.6		0.6		0.6

		0.7		0.7		0.7

		0.9		0.9		0.9

		1		1		1

		0.457		0.457		0.457

		0.457		0.457		0.457

		0		0		0

		2		2		2



In plane of coil

0.5 radius below coil

1 radius below coil

Radial distance from center, meters

Flux, Gauss

Vertical component of field (no iron) of 18" = 0.457 m radius loop

27.5

19.67

9.72

28.5

19.65

9.46

32.3

19.31

8.64

36.1

18.7

8.01

42.6

17.48

7.23

55.3

15.32

6.34

64.4

14.15

5.96

89.9

12.07

5.37

170.5

9.71

4.76

599

8.06

4.36

4035

7.56

4.24

-1302

7.23

4.16

-283

6.42

3.97

-152

5.62

3.77

-101.5

4.86

3.58

-74.6

4.12

3.39

-47.1

2.78

3.02

-28.6

1.11

2.51

-15.9

-0.73

1.75

-7.1

-1.95

0.65

-2.5

-1.51

-0.25

-1.7

-1.18

-0.36

-200

200

0

0



Sheet1

				Gauss

		radial dist		At coil		0.5 r below		1 radius below coil

		0		27.5		19.67		9.72

		0.1		28.5		19.65		9.46

		0.2		32.3		19.31		8.64

		0.25		36.1		18.7		8.01

		0.3		42.6		17.48		7.23

		0.35		55.3		15.32		6.34

		0.37		64.4		14.15		5.96

		0.4		89.9		12.07		5.37

		0.43		170.5		9.71		4.76

		0.45		599		8.06		4.36

		0.456		4035		7.56		4.24

		0.46		-1302		7.23		4.16

		0.47		-283		6.42		3.97

		0.48		-152		5.62		3.77

		0.49		-101.5		4.86		3.58

		0.5		-74.6		4.12		3.39

		0.52		-47.1		2.78		3.02

		0.55		-28.6		1.11		2.51

		0.6		-15.9		-0.73		1.75

		0.7		-7.1		-1.95		0.65

		0.9		-2.5		-1.51		-0.25

		1		-1.7		-1.18		-0.36

		0.457		-200

		0.457		200

		0		0

		2		0






_1692534727.unknown

_1692265041.xls
Chart1

		0

		0

		0.1

		0.25

		0.5

		1

		1.5

		2

		2.5



Distance Z from coil center / radius

Flux/center flux

Fall-off of field along coil axis

1

0.9851853368

0.9130752943

0.7155417528

0.3535533906

0.1706769835

0.0894427191

0.0512263002



Sheet1

				Food

		0		1

		0.1		0.9851853368

		0.25		0.9130752943

		0.5		0.7155417528

		1		0.3535533906

		1.5		0.1706769835

		2		0.0894427191

		2.5		0.0512263002






_1692282813.unknown

_1692266473.unknown

_1691923557.unknown

_1692264907.unknown

_1691922559.unknown

_1691922295.unknown

_1691922306.unknown

_1691922285.unknown

_1689705103.unknown

_1691909797.unknown

_1691911246.xls
Chart1

		1		10

		2		10

		3

		4

		5

		6

		7

		8

		9

		10

		11

		12

		13

		14

		15

		16

		17

		18

		19

		20

		21

		22

		23

		24

		25

		26

		27

		28

		29

		30

		31

		32

		33

		34

		35

		36

		37

		38

		39

		40

		41

		42

		43

		44

		45

		46

		47

		48

		49

		50

		51

		52

		53

		54

		55

		56

		57

		58

		59

		60

		61

		62

		63

		64

		65

		66



H

Vert line

N turns

Relative current

Decrease in current with more turns (R0 = 10 Rt)

1

0

0.9166666667

5

0.8461538462

0.7857142857

0.7333333333

0.6875

0.6470588235

0.6111111111

0.5789473684

0.55

0.5238095238

0.5

0.4782608696

0.4583333333

0.44

0.4230769231

0.4074074074

0.3928571429

0.3793103448

0.3666666667

0.3548387097

0.34375

0.3333333333

0.3235294118

0.3142857143

0.3055555556

0.2972972973

0.2894736842

0.2820512821

0.275

0.2682926829

0.2619047619

0.2558139535

0.25

0.2444444444

0.2391304348

0.2340425532

0.2291666667

0.2244897959

0.22

0.2156862745

0.2115384615

0.2075471698

0.2037037037

0.2

0.1964285714

0.1929824561

0.1896551724

0.186440678

0.1833333333

0.1803278689

0.1774193548

0.1746031746

0.171875

0.1692307692

0.1666666667

0.1641791045

0.1617647059

0.1594202899

0.1571428571

0.1549295775

0.1527777778

0.1506849315

0.1486486486

0.1466666667

0.1447368421



Sheet1

		N		H

		1		1				10		0

		2		0.9166666667				10		5

		3		0.8461538462

		4		0.7857142857

		5		0.7333333333

		6		0.6875

		7		0.6470588235

		8		0.6111111111

		9		0.5789473684

		10		0.55

		11		0.5238095238

		12		0.5

		13		0.4782608696

		14		0.4583333333

		15		0.44

		16		0.4230769231

		17		0.4074074074

		18		0.3928571429

		19		0.3793103448

		20		0.3666666667

		21		0.3548387097

		22		0.34375

		23		0.3333333333

		24		0.3235294118

		25		0.3142857143

		26		0.3055555556

		27		0.2972972973

		28		0.2894736842

		29		0.2820512821

		30		0.275

		31		0.2682926829

		32		0.2619047619

		33		0.2558139535

		34		0.25

		35		0.2444444444

		36		0.2391304348

		37		0.2340425532

		38		0.2291666667

		39		0.2244897959

		40		0.22

		41		0.2156862745

		42		0.2115384615

		43		0.2075471698

		44		0.2037037037

		45		0.2

		46		0.1964285714

		47		0.1929824561

		48		0.1896551724

		49		0.186440678

		50		0.1833333333

		51		0.1803278689

		52		0.1774193548

		53		0.1746031746

		54		0.171875

		55		0.1692307692

		56		0.1666666667

		57		0.1641791045

		58		0.1617647059

		59		0.1594202899

		60		0.1571428571

		61		0.1549295775

		62		0.1527777778

		63		0.1506849315

		64		0.1486486486

		65		0.1466666667

		66		0.1447368421






_1691922153.unknown

_1691909985.unknown

_1691911022.unknown

_1691909846.unknown

_1691679512.vsd

_1691909744.unknown

_1691679615.vsd

_1689881110.unknown

_1691569395.unknown

_1690021857.unknown

_1689705199.unknown

_1689705702.unknown

_1689526690.unknown

_1689613803.unknown

_1689527503.unknown

_1689526651.unknown

